# Product						    Type

## Hot Rod HR 15W-50			High Performance 								Synthetic Engine Oil

________________________________________________________________

Hot Rod HR 15W-50 Synthetic Engine Oil Product Information:

- Unique, full synthetic high performance motor oil.

- Designed for Hot Rod, Vintage, and Classic cars.

- Provides engine protection on the street, on the track, and in your garage.

- Contains the same additive technology used by the US Military for storing and shipping combat equipment worldwide.

- Protects against rust and corrosion during storage and operation.

- Higher levels of zinc antiwear compared to conventional passenger car motor oil to protect older style push-rod and flat tappet engines.

- Synthetic base stocks provide improved cold-start protection compared to conventional motor oils.

- Viscosity typical of SAE 15W-50.

# Typical Physical Characteristics

| PARAMETER | TEST METHOD | VALUE |
| --- | --- | --- |
| Pounds per U.S. gallon at 15.6°C | ---- | 7.15 |
| Specific Gravity at 15.6°C | ASTM D1298 | 0.858 |
| Viscosity at 40°C. cSt | ASTM D445 | 140 |
| Viscosity at 100°C, cSt | ASTM D445 | 19.8 |
| Viscosity Index | ASTM D2270 | 163 |
| Cranking Viscosity at -20°C | ASTM D5293 | 5000 |
| Zinc, wt% | ASTM D4951 | 0.127 |
| Flash Point (PMCC),°C | ASTM D93 | 197 |
| Pour Point, °C | ASTM D97 | -42 |